1. **Operational Steps**
2. Make chip on injection molding machine by using Master Batch in which UV stabilizer/ Sun block is added.
3. Take these chips out and place them in to the sunlight for 7 days.
4. After seven days check the shade difference between the chips of standards and sample.
5. Lighter the chip poor will be the UV stabilizer/ Sun block.
6. **Precautions**

The composition of the chips both the STD and the sample must be same.

|  |  |  |
| --- | --- | --- |
| **Author** | **Review** | **Approval** |
| **Signature** | **Signature** | **Signature** |
| Muhammad Yousaf | Ghulam Murtaza | Ahsan Abid |
| Assistant Manager REC | R&D Manager | General Manager Operational |