|  |  |  |
| --- | --- | --- |
| **Tested Parameters** | **Standard Method** | **PCC** |
| Viscosity Pure (sec,ZC2) | ASTM D1200 | 22 |
| Printing viscosity (sec,ZC2) | ASTM D1200 | 16 |
| L:a:b Values | ASTM E313 | 49.3 : -34.0 : 46.0 |
| Drying time | PCC/LAB/SOP-001 | As per standard |
| Heat Seal at 110°C | PCC/LAB/WI-009 | Ok |
| Tape Test | PCC/LAB/SOP-001 | Ok |
| Scratch Test | PCC/LAB/SOP-001 | Ok |
| Gloss | ASTM D2369 | 61.0 |

Customer: Nisar Art Press

Ink Code: RNP-7243 (Light Green) Date: 22-11-2021

**Shade**

|  |
| --- |
|  |
| **PCC** |

Remarks: Use ink at printing viscosity

\*Viscosity is checked at controlled temperature (25°C). Actual viscosity may vary depending on ambient temperature.

Evaluator: \_\_\_\_\_\_\_\_\_\_\_\_\_\_\_ Approved by: \_\_\_\_\_\_\_\_\_\_\_\_\_\_\_