Customer: Fatima Packaging

Ink Code: FTW-7261(Dark Green against DIC 26974) Date: 31-3-2022

|  |  |  |  |
| --- | --- | --- | --- |
| **Tested Parameters** | **Standard Method** | **Standard** | **PCC** |
| Pure ink viscosity (sec, FC4) | ASTM D1200 | 22 | 27±2 |
| Tape Test | PCC/LAB/SOP-001 | Ok | OK |
| Drying Time | PCC/LAB/SOP-001 | Standard | As per std |

**Shade**

|  |  |
| --- | --- |
|  |  |
| **Standard** | **PCC** |

\*Viscosity is checked at controlled temperature (25°C). Actual viscosity may vary depending on ambient temperature.

Evaluator: \_\_\_\_\_\_\_\_\_\_\_\_\_\_\_ Approved by: \_\_\_\_\_\_\_\_\_\_\_\_\_\_\_

Customer: Fatima Packaging

Ink Code: FTW-6405(Royal Blue against DIC 26870) Date: 31-3-2022

|  |  |  |  |
| --- | --- | --- | --- |
| **Tested Parameters** | **Standard Method** | **Standard** | **PCC** |
| Pure ink viscosity (sec, FC4) | ASTM D1200 | 45 | 45±2 |
| Tape Test | PCC/LAB/SOP-001 | Ok | OK |
| Drying Time | PCC/LAB/SOP-001 | Standard | As per std |

**Shade**

|  |  |
| --- | --- |
|  |  |
| **Standard** | **PCC** |

\*Viscosity is checked at controlled temperature (25°C). Actual viscosity may vary depending on ambient temperature.

Evaluator: \_\_\_\_\_\_\_\_\_\_\_\_\_\_\_ Approved by: \_\_\_\_\_\_\_\_\_\_\_\_\_\_\_

Customer: Fatima Packaging

Ink Code: FTW-7260(Light Green against DIC 21874) Date: 31-3-2022

|  |  |  |  |
| --- | --- | --- | --- |
| **Tested Parameters** | **Standard Method** | **Standard** | **PCC** |
| Pure ink viscosity (sec, FC4) | ASTM D1200 | 15 | 15±2 |
| Tape Test | PCC/LAB/SOP-001 | Ok | OK |
| Drying Time | PCC/LAB/SOP-001 | Standard | As per std |

**Shade**

|  |  |
| --- | --- |
|  |  |
| **Standard** | **PCC** |

\*Viscosity is checked at controlled temperature (25°C). Actual viscosity may vary depending on ambient temperature.

Evaluator: \_\_\_\_\_\_\_\_\_\_\_\_\_\_\_ Approved by: \_\_\_\_\_\_\_\_\_\_\_\_\_\_\_

Customer: Fatima Packahging

Ink Code: FTW-6003(Blue against DIC 26980) Date: 31-3-2022

|  |  |  |  |
| --- | --- | --- | --- |
| **Tested Parameters** | **Standard Method** | **Standard** | **PCC** |
| Pure ink viscosity (sec, FC4) | ASTM D1200 | 26 | 25±2 |
| Tape Test | PCC/LAB/SOP-001 | Ok | OK |
| Drying Time | PCC/LAB/SOP-001 | Standard | As per PCC std |

**Shade**

|  |  |
| --- | --- |
|  |  |
| **Standard** | **PCC** |

\*Viscosity is checked at controlled temperature (25°C). Actual viscosity may vary depending on ambient temperature.

Evaluator: \_\_\_\_\_\_\_\_\_\_\_\_\_\_\_ Approved by: \_\_\_\_\_\_\_\_\_\_\_\_\_\_\_