Customer: FM Packages

Ink Code: AQF-6370 (Blue) Date: 28-4-2022

|  |  |  |  |
| --- | --- | --- | --- |
| **Tested Parameters** | **Standard Method** | **Standard** | **PCC** |
| Viscosity Pure (sec, FC4) | ASTM D1200 | 44 | 16±2 |
| Printing Viscosity (sec, FC4) | ASTM D1200 | 44 | 16 |
| L:a:b value | ASTM E313 | 22.4 : 10.6 : -14.1 | 20.5 : 12.1 : -13.5 |
| Drying time | PCC/LAB/SOP-001 | Standard | As per PCC Std |
| pH | PCC/LAB/WI-014 | 8.75 | 7.8-8.5 |
| Rub Test | PCC/LAB/WI-016 | Standard | As per PCC Std |

**Shade**

|  |  |
| --- | --- |
|  |  |
| **Standard** | **PCC** |

\*Viscosity is checked at controlled temperature (25°C). Actual viscosity may vary depending on ambient temperature.

Evaluator: \_\_\_\_\_\_\_\_\_\_\_\_\_\_\_ Approved by: \_\_\_\_\_\_\_\_\_\_\_\_\_\_\_