Customer: Lahore Sack

Ink Code: AQF-7259-N (Green) Date: 31-3-2022

|  |  |  |  |
| --- | --- | --- | --- |
| **Tested Parameters** | **Standard Method** | **Standard** | **PCC** |
| Viscosity Pure (sec, FC4) | ASTM D1200 | 17 | 26±2 |
| Drying time | PCC/LAB/SOP-001 | Standard | As per Std |
| pH | PCC/LAB/WI-014 | 8.7 | 7.8-8.5 |
| Rub Test | PCC/LAB/WI-016 | Standard | As per Std |

**Shade**

|  |  |
| --- | --- |
|  |  |
| **Standard** | **PCC** |

\*Viscosity is checked at controlled temperature (25°C). Actual viscosity may vary depending on ambient temperature.

Evaluator: \_\_\_\_\_\_\_\_\_\_\_\_\_\_\_ Approved by: \_\_\_\_\_\_\_\_\_\_\_\_\_\_\_